Home < Material Details < PC Tolerances
PC Tolerances

Magnetic Tolerance. Material (Mix No.); -2; -8; -14; -18; -19; -26; -28; -30; -33; -34; -35; -38; -40; -45; -52; -267; -275. AL Tolerance; ±5%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; ±10%; +35% -25%; +35% -25%. The cores are manufactured to the AL values listed; the permeability for each material is for reference only. In all cases, the AL values are based on a peak AC flux density of 10 guass (1mT) at a frequency of 10kHz. Measurements made under other conditions will produce results in accordance with the magnetic curves shown in the Percent Initial Permeability vs. Peak AC Flux Density Graph. The toroidal cores are tested with an evenly-spaced full single-layer winding in order to minimize leakage effects. Iron powder cores tested with a small number of turns which are not evenly distributed will produce higher inductance readings than expected. The E cores are tested with 100 turns. The Magnetic Characteristic curves shown are have a typical tolerance of ±10%. The curves on Core Loss characteristics have a typical tolerance of ±15%..

Dimensional Tolerances (inches). TOROIDS*; OD; ID; Ht; TOROIDS*; OD; ID; Ht. T16-T20; ±.010; ±.010; ±.010; T150-T225; ±.025; ±.025; ±.030. T25-T38; ±.015; ±.015; ±.020; T249-T400; ±.030; ±.030; ±.030. T40-T72**; ±.020; ±.020; ±.020; T520-T650; ±.050; ±.050; ±.050. T44-T72**; ±.020; ±.020; ±.020. T80-T141; ±.020; ±.020; ±.025. -. COMPOSITE*; OD; ID; Ht; COMPOSITE*; OD; ID; Ht. ST50; ±.015; ±.015; ±.020; ST150; ±.040; ±.030; ±.030. ST83-ST102; ±.030; ±.020; ±.025; ST200; ±.050; ±.040; ±.040. -. BUS BAR*; A; B; D; E; L. HS300-HS400; ±.015; ±.020; ±.005; ±.005; ±.020. -. U CORES; A; B; C; E; F; G. U61-U80; ±.010; ±.010; ±.010; ±.010; ±.010; ±.010. U350; ±.020; ±.020; ±.015; ±.020; ±.015; ±.030. -. E CORES; A; B; C; D; F; G; MAX GAP***. E49-E118; ±.010; ±.010; ±.005; ±.007; ±.005; ±.007; .0015. E125-E162; ±.015; ±.015; ±.007; ±.010; ±.007; ±.010; .0015. E168-E225; ±.015; ±.015; ±.010; ±.010; ±.007; ±.010; .0020. E305-E450; ±.030; ±.030; ±.015; ±.020; ±.015; ±.020; .0030. E610; ±.040; ±.040; ±.025; ±.030; ±.025; ±.030; .0050. -. EF CORES; A; B; C; D; E/F; G; MAX GAP***. EF60-EF80; ±.010; ±.010; ±.005; ±.010; ±.005; ±.007; .0030. -. EM CORES; A; B; C; D; G; H; MAX GAP***. EM145; ±.015; ±.015; ±.010; ±.020; ±.010; ±.015; .0020. EM168-EM220; ±.015; ±.015; ±.010; ±.020; ±.010; ±.015; .0030. -. PLAIN CORES; OD; L. Pxx24-Pxx40; +.000/-.005; ±.015. Pxx48-Pxx76; +.000/-.005; ±.020. -. HOLLOW CORES; OD; ID; L. Hx10-Hx12; +.000/-.005; +.005/-.000; ±.010. Hxx14-Hxx20; +.000/-.005; +.005/-.000; ±.015. Hxx21-Hxx25; +.000/-.005; +.005/-.000; ±.020. -. DISCS; OD; CB; ID; T. D45-D80; +.000/-.010; +.005/-.000; +.005/-.000; ±.007. -. *Tolerance includes coating **Gap per piece; ** OD for T50-8/90 and T50-8B/90 is + 025/- .015.

About Us | What We Do | Contact Us | Samples | Catalog | Thermal Aging | Parts | Materials | Software | Home